## Slide 1: Exam Slides
Cleanroom Fabrication – Joel von Rotz

## Slide 2: Photolithography
Lithography
Photolithography
  Photoresist
  Process
Mask Aligner
  Exposure Systems
Practical Limit: ~0.7-1μm
Practical Limit: <0.1μm
Notes: Lithography
  Types of Lithography: Photolithography ; Electron beam lithography (EBL) ; Nanoimprint lithography (NIL)
  What is Lithography? Used to create a pattern on the surface of a substrate (such as a silicon wafer)
Photolithography
  Basic Photolithography Process
    CAD System -> draw layout, simulation, design rule checking
    Mask Making -> Using electron gun to engrave the designed pattern into the mask or onto the quartz glass
    Wafer Expose -> the photolithography step of applying the mask to the wafer
  Steps
  UV Light
    To draw the patterns from the mask onto the wafer, a good enough light source is required. Nowadays UV light is used to to it's smaller wavelength, which allows for better pattern resolutions on the wafer.
      Mercury high-pressure arc lamp
    Diffraction
      As light bends around edges, it diffracts from its "ideal" path, also called diffraction.
      Using masks, the light diffracts more, the bigger the gap is. By reducing (for example with contact printing), the diffraction can be mitigated.
    1:1 Printing
      Under 1:1 printing is a exposure system, which does not use magnifying glasses to scale the mask somehow.
    Exposure Systems
      Contact: mask directly placed on top wafer (limit: ~0.7-1μm)
      Proximity: between mask and wafer is a gap (bigger gap, more diffraction)
      Projection: Mask scaled down to final size (limit: <0.1μm)
  Tools
    Mask Aligner
      The Hg (mercury) lamp emits an unevenly spread UV light -> Using mirrors to correct the light
      To align a mask with a previously etched wafer, it needs to align with alignment mark
    Photoresist (RESIN)
        Positive R: curved edges, masked area is not soluble
        Negative R: overhang edges, exposed area is soluble
      Image Reversal (first exposed area is soluble!
      Resist Adhesion
        To make the wafer more suitable for PR, adhesion promoter is applied onto the wafer using a HMDS
        HMDS - Hexamethyldisilane -> Applied in vapour form in vacuum chamber
E-Beam Litho: Direct Writing ; electron optics (coils) ; high resolution (<100mm) ; low throughput
Nanoimprint Lithography: Thermal NIL ; UV NIL

## Slide 3: Deposition of thin films
Difference between CVD & PVD
CVD: LPCVD
PVD: E-Beam Evaporation
CVD
Wafer
Vacuum Chamber
PVD
Microbalance
Notes: CVD
  Transport of reactants to the deposition region.
  Transport of reactants from the main gas stream through the boundary layer to the wafer surface.
  Adsorption of reactants on the wafer surface.
  Surface reactions, including: chemical decomposition or reaction, surface migration to attachment sites (kinks and ledges); site incorporation; and other surface reactions (emission and redeposition for example)
  Desorption of byproducts.
  Transport of byproducts through boundary layer.
  Transport of byproducts away from the deposition region.
  APCVD: Atmospheric Pressure CVD + high temperatures
    The above system contains RF induction coils to control the temperature of the chamber.
    The wafers are placed on top a graphite susceptor, which is slightly angled so all wafers are exposed.
    Gas inserted into chamber, reaction happens, gas goes out through vent.
  LPCVD: Low Pressure CVD + high temperature
    Reduced pressures reduces unwanted gas-phase reactions and improve film uniformity across the wafer.
  Plasma Enhanced CVD (PECVD): low temperature vacuum thin film deposition process with a very strong position in the semiconductor industry
    Plasma consists of electrons, ionized molecules, neutral molecules, neutral and ionized fragments of broken-up molecules, excited molecules and free radicals.
    Free radicals are electrically neutral species that have incomplete bonding and are extremely reactive. (e.g. SiO, SiH3, F)
    The net result from the fragmentation, the free radicals, and the ion bombardment is that the surface processes and deposition occur at much lower temperatures than in non-plasma systems.
  Epitaxial Growth
  CVD Modelling
    : Mass Transfer Flux, Step 2
    : Surface Reaction Flux, Steps 3-5
    The growth rate can be adjusted via pressure. Lowering the pressure reduces the gas-density and therefore increases the deposition rate.
PVD
  2 general types: Evaporation and Sputtering
  Evaporation
    Compared to CVD, this does not use any gases and operates in vaccuum.
    Thickness Uniformity
      As the wafer is not curved, there will be slightly different thicknesses on the wafer, due different evaporation rates. If uniformity is important, increase the substrate distance, which unfortunately reduces the rate () and might require a bigger chamber.
    Sidewall Coverage
    Measuring the Deposition Rate during Deposition
      A quartz crystal microbalance (quartz crystal between two electrodes, oscillation frequency depends on the mass) can be used to measure the thickness of the deposited material on the wafer.
  E-Beam Evaporation: Electron Gun  very precise, but pricey
  Thermal Evaporation: Resistive Heater  can cause contamination from crucible
  Sputtering
    Sputtering uses an electric field and a noble gas, such as argon, to take material from the target plate or cathode to the wafers, which are on top the anode.
  DC Sputtering
    DC Sputtering allows only conductive material to be deposited!
    Cathode negative, anode positive
    Neutral Argon ionized via forceful collision
    Charged Argon moves towards anode, bringing vaporized target with
    Magnetron traps electrons over negative cathode/target  not free to bombard the substrate, increasing faster deposition
    Voltage Distribution
  RF Sputtering
    RF Sputtering can deposit most materials (conductive and non-conductive
    Cathode and Anode are RF charged
    Over time, positive ions are accumulated on target surface
    Enough positive charge, complete secession happens  discharged for coating
    Adv. RF diffuses entire chamber  charged is “cleaned” off
    Disadv. does not acquire great charge buildup due to being discharged each half cycle and becoming insulated.
    Voltage Distribution
CVD
  Transport of reactants to the deposition region.
  Transport of reactants from the main gas stream through the boundary layer to the wafer surface.
  Adsorption of reactants on the wafer surface.
  Surface reactions, including: chemical decomposition or reaction, surface migration to attachment sites (kinks and ledges); site incorporation; and other surface reactions (emission and redeposition for example)
  Desorption of byproducts.
  Transport of byproducts through boundary layer.
  Transport of byproducts away from the deposition region.
  APCVD: Atmospheric Pressure CVD + high temperatures
    The above system contains RF induction coils to control the temperature of the chamber.
    The wafers are placed on top a graphite susceptor, which is slightly angled so all wafers are exposed.
    Gas inserted into chamber, reaction happens, gas goes out through vent.
  LPCVD: Low Pressure CVD + high temperature
    Reduced pressures reduces unwanted gas-phase reactions and improve film uniformity across the wafer.
  Plasma Enhanced CVD (PECVD): low temperature vacuum thin film deposition process with a very strong position in the semiconductor industry
    Plasma consists of electrons, ionized molecules, neutral molecules, neutral and ionized fragments of broken-up molecules, excited molecules and free radicals.
    Free radicals are electrically neutral species that have incomplete bonding and are extremely reactive. (e.g. SiO, SiH3, F)
    The net result from the fragmentation, the free radicals, and the ion bombardment is that the surface processes and deposition occur at much lower temperatures than in non-plasma systems.
  Epitaxial Growth
  CVD Modelling
    𝐹_1: Mass Transfer Flux, Step 2
    𝐹_2: Surface Reaction Flux, Steps 3-5
    The growth rate can be adjusted via pressure. Lowering the pressure reduces the gas-density and therefore increases the deposition rate.
PVD
  2 general types: Evaporation and Sputtering
  Evaporation
    Compared to CVD, this does not use any gases and operates in vaccuum.
    Thickness Uniformity
      As the wafer is not curved, there will be slightly different thicknesses on the wafer, due different evaporation rates. If uniformity is important, increase the substrate distance, which unfortunately reduces the rate () and might require a bigger chamber.
    Sidewall Coverage
    Measuring the Deposition Rate during Deposition
      A quartz crystal microbalance (quartz crystal between two electrodes, oscillation frequency depends on the mass) can be used to measure the thickness of the deposited material on the wafer.
  E-Beam Evaporation: Electron Gun  very precise, but pricey
  Thermal Evaporation: Resistive Heater  can cause contamination from crucible
  Sputtering
    Sputtering uses an electric field and a noble gas, such as argon, to take material from the target plate or cathode to the wafers, which are on top the anode.
  DC Sputtering
    DC Sputtering allows only conductive material to be deposited!
    Cathode negative, anode positive
    Neutral Argon ionized via forceful collision
    Charged Argon moves towards anode, bringing vaporized target with
    Magnetron traps electrons over negative cathode/target  not free to bombard the substrate, increasing faster deposition
    Voltage Distribution
  RF Sputtering
    RF Sputtering can deposit most materials (conductive and non-conductive
    Cathode and Anode are RF charged
    Over time, positive ions are accumulated on target surface
    Enough positive charge, complete secession happens  discharged for coating
    Adv. RF diffuses entire chamber  charged is “cleaned” off
    Disadv. does not acquire great charge buildup due to being discharged each half cycle and becoming insulated.
    Voltage Distribution

## Slide 4: Etching
What is Etching?
  Wet & Dry Etching
Dry & Wet Etching
  Selectivity
  Etch Anisotropy
Dry Etching
  Plasma Etch - Physical
Surface Atom Density:
Etching Rate:
Notes: Etching: is process of removing material through various methods such as dry and wet etching.
  Wet Etching
    Chemical Process
    Wafers are immersed in liquid etchant solution and dried afterwards.
  Dry Etching
    Physical & Chemical Process
    Wafers are exposed to gas-phase etchants in the form of a plasma (plasma etching)
Wet vs. Dry Etching
  Selectivity: to compare the etch rate differences between two materials  relative characteristic.
Wet Etching?
  Etch Rate Table
    The etch rate table provides an overview on etch rates of different etchants on different materials.
    Noteworthy Etchants: - Silicon Etchant (126 HNO₃ ; 60 H₂O ; 5 NH₄F) -> etches silicon and not photoresist - KOH (1 KOH, 2 H₂O by weight) -> Crystallographic Etching <100> Silicon - Acetone (C₃H₆O) -> used to remove Photoresist
  Crystal Directions and Planes
    Equivalent directions . : , , , , …
    Specific plane . The specific direction is normal to .
    Equivalent planes
  Crystallographic Etching
    As silicon is a crystalline material, etching rate on more densely packed surfaces are lower than on that of loosely packed surfaces.
  Different Etch Rates
    Atoms within the and faces possess two dangling bonds, two bonds into the crystal (less binding energies)
    Atoms within the faces possess only a single dangling bonds (larger binding energies)
  Etch Anisotropy
    Different plane directions provide vastly different etch rates (100 vs 111), therefore a pyramidic shape gets etched with a bit of isotropic etching.
Dry Etching
  Physical & Chemical Etching in a Plasma
    Chemical etching (radical species): isotropic, selective
    Physical etching (ions): anisotropic, less selective
    Ion-enhanced etching: anisotropic, selective
  Chemical Etching
  Physical Etching
  Ion Enhanced Etching 
    The chemical and physical components can act in a synergistic manner
    Etch profiles can be very anisotopic, and selectivity can be good.
  Plasma Etching Types

## Slide 5: Silicon - Si
What is Silicon?
Crystal Structure
Electrical Properties
  Bandgap
  Doping
Notes: What is Silicon?
  Si-Atom: 2 + 8 + 4 = 14 Atoms
    4 Valence Electrons -> 4 chemical bonds possibile
    Carbon structure allows for wafers with specific "cut directions"
  Why Silicon? – Abundant element (~26%) ; Simple Purification ; Good crystal quality
What can it be used for?
  Integrated Circuits -> Computers, Microcontrollers, logic gates, amplifiers, etc.
  Micro-ElectroMechanical Systems
Crystal Structures: cubic (1 atom per unit cell), BCC (2), FCC (4)
Crystal Directions and Planes: The directions are noted in the Miller Index form
Silicon Unit Cell: 2 FCC Sub Cells ; Shift: 1/4 body diagonal
Electrical Properties
  Bandgap (Electron Energy ; Conduction & Valence Band)
    Conductor (Overlap) ; Insulator (Separation) ; Semiconduction (smaller gap + can be changed)
    thermal excitations responsible for electron transport from valence to conduction. If too cold (), transport not possible
    Intrinsic carrier concentration concentration of the ‘free’ carriers for transport.
  Doping (intentional introduction of impurity to alter property)
    The resistivity of a semiconductor material generally decreases as the doping concentration increases.
    p-doped uses Boron (introduces holes)
    n-doped uses Phosphorus (introducing excess electrons)
What is Silicon?
  Si-Atom: 2 + 8 + 4 = 14 Atoms
    4 Valence Electrons -> 4 chemical bonds possibile
    Carbon structure allows for wafers with specific "cut directions"
  Why Silicon? – Abundant element (~26%) ; Simple Purification ; Good crystal quality
What can it be used for?
  Integrated Circuits -> Computers, Microcontrollers, logic gates, amplifiers, etc.
  Micro-ElectroMechanical Systems
Crystal Structures: cubic (1 atom per unit cell), BCC (2), FCC (4)
Crystal Directions and Planes: The directions are noted in the Miller Index form
Silicon Unit Cell: 2 FCC Sub Cells ; Shift: 1/4 body diagonal
Electrical Properties
  Bandgap (Electron Energy ; Conduction & Valence Band)
    Conductor (Overlap) ; Insulator (Separation) ; Semiconduction (smaller gap + can be changed)
    thermal excitations responsible for electron transport from valence to conduction. If too cold (0𝐾), transport not possible
    Intrinsic carrier concentration concentration of the ‘free’ carriers for transport.
  Doping (intentional introduction of impurity to alter property)
    The resistivity of a semiconductor material generally decreases as the doping concentration increases.
    p-doped uses Boron (introduces holes)
    n-doped uses Phosphorus (introducing excess electrons)

## Slide 6: Thermal Oxidation of Silicon
SiO2
Si
What is Thermal Oxidation?
  Wet & Dry Oxidation
Silicon Dioxide
Deal-Grove Model
Thermal Oxide
Notes: What is the Thermal Oxidation used for?
  By heating up the wafer (to 800°C-1200°C) and supplying O₂ or H₂O creates a SiO₂ layer on the Si layer
    Dry: Si + O₂ -> SiO₂
    Wet: Si + H₂O -> SiO₂ + 2 H₂
    Volume Expansion Factor: 2.2
    consumes Silicon
    Deal-Grove Model shows the concentration amount depending on the thickness of the material. Si is zero, due to turning into SiO₂. The thicker SiO₂ gets, less concentration can reach Si.
    The flux rates (analogy current in series resistor circuit) are the same
What is the oxidation master curve?
What needs to be considered when using Thermal Oxidation?
  Volume Expansion
    As with any other physical material, it expands with increasing temperature. It expands by a factor of 2.2 of it's volume. Meaning a silicon cube expands to .
How does Thermal Oxidation work?
  To etch structures reliably into Si-Wafers, they are treated in a oxidation furnace.
    Wafer are loaded into boat (with dummy wafers outside for better temperature isolation for the other wafers)
    Wafers get heated up
    Treatment gas is inserted (such as O₂, H₂O) and diffuses with the silicon and reacts, resulting into SiO₂
How is the thickness of SiO₂ measured?
  Profilometer / AFM
    An Atomic Force Microscope uses a tiny needle, laser and photodiode to detect topological changes on the sample.
  Optical measurements such as Interferometry, Ellipsometry, Visual inspection
    An Ellipsometer measures the phase shift of a laser shun into the wafer. Two reflections will occur and are timely differently measured (phase shift).
Silicon Dioxide: A product of thermal oxidation
  Acts as a insulator
    Is used for example for oxide layer in a MOSFET.
  While silicon has a diamond structure, thermally grown silicon dioxide is amorphous (meaning no crystalline structure)
  Through the thermal procedure, the structure is as mentioned before amorphous, meaning no rigid crystalline structure. While it is a faster oxidation, it leads to no nice structures